| SPECIFICATION TEXT |
| --- |
| PRODUCT | LVL (Laminated Veneer Lumber) | DATE | 11/06/2015 |
| CE CLASS | - | EN STANDARD | EN 14374 |

DESCRIPTION

Water-repellent, multiply, structural construction boards

SpanoTech LVL/Laminated Veneer Lumber is a synthetic wood formed with certified, resinous wood veneers (pine, fir, spruce) obtained by peeling. The 3 mm thick veneers are joined together using scarf and staggered joints. After being joined lengthways, the veneer sheets are hot-glued together under high pressure using a phenol-formaldehyde adhesive (E1) to form large panels (billets) which are then cut to obtain the final format as planks or joists of different sections. The minimum number of veneer sheets is 7 (total minimum thickness 21 mm).

SpanoTech LVL/Laminated Veneer Lumber type R has all the veneer sheets oriented lengthwise.

SpanoTech LVL/Laminated Veneer Lumber type X has 20 % of the veneer sheets oriented crossways for greater dimensional stability.

The density (5 % fractile) is ± 480 kg/m³.

The moisture content when leaving the factory is between 8 % and 12 %.

The manufacturing tolerances are:

- thickness from -1.5 to + 1.5 mm

- width from -1 to + 1 mm < 200 mm and -2 to + 2 mm for 200 to 600 mm

- maximum 1.5 mm curvature per metre

- length from - 5 to + 5 mm

SpanoTech LVL/Laminated Veneer Lumber complies with EN 14374.

The uses for SpanoTech LVL/Laminated Veneer Lumber are:

- structural joists

- posts/columns

- elements for complex structures (roof truss, for example)

- components for timber frame

- planking

- I-joist flanges

- components for different structural caissons

- façade elements

- components for carpentry work

- components for formworks

SpanoTech LVL/Laminated Veneer Lumber can be used without special treatment in service classes 1 and 2 in accordance with EN 1995-1-1. In the case of service class 3 usage, SpanoTech LVL/Laminated Veneer Lumber will receive suitable preservation treatment.

The dimensions of the SpanoTech LVL/Laminated Veneer Lumber elements must be based on the characteristics listed in the table below and be in accordance with the Eurocode 5 calculation standard.

SpanoTech LVL/Laminated Veneer Lumber joists and planks must be stored in a dry and ventilated place. They must be stacked flat and raised off the ground to avoid any contact with stagnant or seeping water or mud. If necessary, they must be protected by a tarpaulin to ensure good ventilation until they are installed.

During installation, precautions need to be taken to avoid direct and extended contact of the joists with water (take out of the water/air at the construction site as quickly as possible).

STANDARD DIMENSIONS

Type R

Thickness: 30-33-36-39-45-51-63-75-90-100 mm

Width: 120-150-160-200-220-240-260-300-360-400-420-450-500-600-1250 mm

Length: 4-6-8-8.5-9-9.5-10-10.5-12-12.5-13-13.5 m

Type X

Thickness: 27-30-33-36-39-45-51-63-75 mm

Width: 120-150-160-200-220-240-260-300-360-400-420-450-500-600-1250 mm

Length: 4-6-8-8.5-9-9.5-10-10.5-12-12.5-13-13.5 m

Other formats (thickness-length-width) are possible within the limits of the industrial production process.

TECHNICAL SPECIFICATIONS

|  | Reference | Value |
| --- | --- | --- |
| Declaration of Performance (DoP) | DOPUltraLAMRLVLv1 |  |
| Product type |  | LVL(Laminated Veener Lumber) |
| Characteristic design qualities |  |
| Characteristic | Orientation |  |  | Prestation |
| Calculation value density | fraction 5% | Ρ0,05 | kg/m³ | 480 |
| Bending strength | On surface | f m, o , d | N/mm² | 50 |
|  | Along edges | f m, o , d | N/mm² | 48 |
|  | Tolerance parameter |  |  | 0,15 |
| Tensile strength | Parallel with fiber | f t,o, d | N/mm² | 36 |
|  | Perpendicular to fiber, along edges | f t,90, d | N/mm² | 0,9 |
|  | Perpendicular to fiber, on surface | f t,90, d | N/mm² | NDP |
| Compressive strength | Parallel with fiber | f c, o , d | N/mm² | 40 |
|  | Perpendicular to fiber, along edges | f c,90, d | N/mm² | 7,5 |
|  | Perpendicular to fiber, on surface | f c,90, d | N/mm² | 3,8 |
| Shear force | Parallel to fiber (average) | f v, d | N/mm² | 3,2 |
|  | Along edges | f v, d | N/mm² | 4,6 |
| Elasticity modulus | Parallel to fiber (average) | Eo, mean | N/mm² | 14000 |
|  | Parallel to fiber (5% fractile) | Eo, 0.05 | N/mm² | 12000 |
|  | Perpendicular to fiber, along edges (average) | E90,mean |  | NDP |
|  | Perpendicular to fiber, on surface (average) | E90,mean |  | NDP |
| Shear modulus | Along edges (average) | G mean | N/mm² | 500 |
|  | On surface (average) | G mean | N/mm² | 500 |
| Fire reaction class |  |  |  | D-s1,d0 |
| Formaldehyde emission class |  |  |  | E1 |
| Durability class |  |  |  | 4 |